## Slide 1: Verification Analysis of a Plug Assist Thermoformed Part through Computer Simulation.
Or “Virtual Thermoforming”

## Slide 2: Outline
Background on simulation at Fabri-Kal
Current research
Results
Next steps

## Slide 3: Thermoforming - It’s all about distribution

## Slide 4: Factors Affecting Distribution
Sheet temperature (and temperature profile)
Rate of deformation (plug speed)
Timing of vacuum/air (ballooning,billow forming)
Plug assist geometry
Plug material properties (friction, thermal properties)

## Slide 5: Plug geometry is a big reason they refer to thermoforming as an art!

## Slide 6: Fabri-Kal began using simulation software (see last photo)
Goal: Optimize plug shapes in the design stage
Benefits:
  Reduced development time
  Lower development costs
  Better understanding/optimization

## Slide 7: Experience with Simulation
Took time to develop the “right” parameters
Directionally correct
Excellent visualization tool
Good cause/effect with plug designs

## Slide 8
Before plug modification After plug modification

## Slide 9: Research
As we worked, we wanted to better understand the effect of:
  Material properties
  Temperature
  Friction

## Slide 10: Joined research initiative
Noel Tessier, CMT Materials, Inc
Bernard Hegeman, IKP, University of Stuttgart
Dr. Karel Kouba and Petr Novotny, Accuform
Fabri-Kal Corp.

## Slide 11: Research objectives
Identify/quantify the effect of various plug materials
Provide friction data for model
Refine material characterization for F-K’s HDPE material

## Slide 12: Research Step 1
IKP to produce force/displacement curves
  3 select temperatures
  Various plug materials (CMT and other)
  selected strain rates (plug speeds)

## Slide 13
IKP test fixture schematic

## Slide 14
Technical Data:
velocity up to 4 m/s
temperature -80 to +250°C
maximum force 20 kN
draw depth of 120mm
Measurement Performance:
specimen thickness 0.1- 5 mm
various clamping and plug diameters
constant heating with circulating air
Thermoforming Equipment at IKP - Universal Testing Machine MFL-Systems

## Slide 15: Step 2
Accuform to convert data to K-BKZ model
  produce new model for HDPE material
  attempt to identify coefficient of friction
Note: the experimental results published at ANTEC ‘02

## Slide 16: Step 3
Fabri-Kal to compare simulation using the new parameters to actual part

## Slide 17
Actual part vs. simulation using original material

## Slide 18
Actual part vs. simulation using modified material

## Slide 19
Actual part vs. new material, modified friction and temperature.

## Slide 20: Results
Difficult to separate material properties from the frictional effect
May not be the best method to determine friction effect
HDPE was a more difficult material to determine friction effect
Demonstrated definite correlation between plug material and force/deformation curves as well as distribution
Coefficient of friction appears much higher than earlier thought (1.75 vs 1.0)

## Slide 21: Next steps
Explore other options to obtain friction data
Friction data can then be combined with force/deformation curves to yield better material characterizations

## Slide 22: DMA friction data

## Slide 23: Thanks to:
Noel Tessier
Benard Hegemann
Dr. Kouba
Petr Novotny
Gary Bryant