Improving our Industry through Technical Developments: 
the next step:
 a European programme sponsored by the EEC

B. Hegemann and P. Eyerer

IKP, Institute for Polymer Testing and Polymer Science, University of Stuttgart,

Pfaffenwaldring 32, 70569 Stuttgart, Germany, hegemann@ikp.uni-stuttgart.de

Abstract

Thermoforming is a widely used process to produce plastic parts for various applications. Production is very cost-effective with regard to tooling and machinery costs and achieves high output rates. To optimise the thermoforming process, computer simulations with finite-element methods (FEM) are carried out. However, a big problem with thermoforming is that precise material data is not available and the simulations are very expensive and time-consuming procedure.

The target of this project, funded by the EEC, is to develop low-cost measurement apparatus to measure material behaviour and fitting software for the precise characterisation of thermoforming materials. It is aimed at an official test procedure, which can also be used for quality assurance. With the measurement results, a data base will be developed for storing all relevant material data to be used for process optimisation and for the design of new polymer products and tools.

In co-operation with the Institute for Polymer Sciences IKP of the University of Stuttgart as a RTD performer, the SME proposers Wagner GmbH (Germany), Accuform Ltd. (Czech Republic), the thermoformers Jacob Kunststofftechnik (Germany) and APT Prototypentechnologie (Austria), intend to develop a measuring apparatus and fitting software for thermoforming material characterisation.

Introduction

The IKP at the University of Stuttgart’s major knowledge and competence is in developing measurement techniques and measuring mechanical properties of polymers. Beside this, plenty of research has been done on material behavior investigations, dependent on both temperature and deformation velocity.

The new task is to develop a measurement technique that allows thermoformers to investigate polymer material behavior by themselves with respect to the following aspects:

Firstly, a method has to be developed, which enables the possibility of measuring the mechanical behavior of polymers close to the real thermoforming process. Secondly, a routine has to be found allowing thermoformers to derive material parameters for thermoforming simulation software. Thirdly material quality control should be possible.

The following paper describes the existing laboratory scale measurement device and the method of gaining parameters and influences, which can be revealed with this measurement technique.

Measurement Device

For measuring material properties, a device has to be developed which can measure the biaxial deformation behavior, which is both temperature and velocity dependent. The present laboratory device has the following specifications:

For deformation, a sheet is located in a round clamping device. After it is clamped tightly, the complete device (clamp, plug and sample) is heated up in the temperature chamber to the defined temperature, which is between –60°C and +200°C, with an average tolerance of  2°C. The piston, with plug attached, impacts the sample at the predefined velocity and deforms the sample with a maximum draw depth of 120 mm. During deep drawing, force is measured by a load-cell and displacement is measured by piston travel. In addition, the time is given by an internal trigger device (Figure 1). Force, time and deformation results are gathered and evaluated with appropriate software. Results of the complete deep-drawing process are force-deformation-graphs.

Figure 1: Deformation Device in Principle

Thermforming Simulation Parameters

Force-Deformation Graphs

For identifying the material’s properties and the parameters for material models such as K-BKZ and PTT, tests have to be executed at different temperatures to derive the temperature sensitivity of the material. The temperatures should be the processing temperature (Tp) of the material and two further temperatures close to Tp to fulfill the requirements of either the Arrhenius or WLF-equation [1].

To identify the time/velocity dependence, a set of at least three tests has to be executed at different velocities, one of which should be close to the thermoforming process velocity. Figure 2 and 3 show typical force-deformation curves generated at different temperatures and velocities. According to the theoretical behavior of polymers [2], it is proved that the maximum force increases with increasing velocity and decreases with temperature.

These force-deformation-data can now be fitted into stress-strain-data by ‘reverse engineering’.

| Figure 2: Temperature Dependency of PP@20mm/s | Figure 3: Velocity Dependency of PP@164°C |
| --- | --- |

Reverse-Engineering Method

The kernel of the reverse-engineering method is a comparison between the real and the simulated process. Therefore, the biaxial measurement device is modeled by simulation software (T-Sim®). With this, the plug geometry, sheet geometry, material properties and the testing conditions such as temperature and velocity, are modeled and defined. After the testing conditions are described, a first simulation can be run and the force-deformation data can be generated.

Due to the fact that caused by real executing the deformation test at the laboratory device, a set of nine temperature and velocity dependent force-deformation-curves already exist. Now a method, the so-called “reverse-engineering” method, can be used. This method fits the simulated curves as close as possible to the measured curves by means of the least square method (LSM) (Figure 4) [3].

After fitting both, simulated and measured curves and deriving the optimum results by LSM, the parameters for the K-BKZ model can be extracted and the material is accurately described for thermoforming simulation.

Figure 4: “reverse-engineering” Schema

Material Data File

The parameters, as a result of the reverse-engineering method, are the K-BKZ parameters of the tested material. These are the relaxation spectra (pairs of time and modulus), the Wagner damping functions and the strain-hardening effect of the material. In addition, the shift parameters for either the Arrhenius or the WLF equation are available. For a complete description the thermal properties ,  and cp are necessary, but they are mostly taken from literature or provided by material suppliers.

This data file is a special file that can be easily implemented into T-Sim software and the simulation process can begin.

Material Quality Control

A third major focus of the project is to enable a material quality control system which allows thermoformers to identify the material properties and, especially, changes in material properties within the same material group.

Therefore, a first reference measurement of the “good thermoformable” material at pre-defined temperatures and velocities has to be made. Saving this first material data, including the settings in an internal database, opens the possibility of comparing each new material batch with the reference. An explanation of curve interpretation and an extensive database will allow the thermoformer to proof batch changes and the reason behind.

Some characteristics observed by material changes are described in the following:

Changes due to material modification

Polymer materials are not, in most cases, homo-polymers, meaning they are modified with special additives to improve their initial properties with the focus on; e.g. transparency, formability or material strength. Figure 5 shows a set of curves where a certain percentage of modifier was added to the homo-polymer polypropylene. This modifier was especially developed to improve the transparency of polypropylene.

Figure 5: PP with Different Amounts of Modifier

Changes due to internal orientations

Identifying processing treatments of the initial sheet material, investigations revealed a curve characteristic for internal orientations in the material. Figure 6 shows curves of two different clamping methods: The first sheet was heated up in an unclamped state (warm clamped); the second was heated up in a clamped state (cold clamped) and, therefore, the sample could not move in any direction.

It can be seen that the cold clamped sample shows a peak in the slope. This phenomenon is supposed to come from internal orientations due to material processing. According to the fact that the material cannot move during heating the internal stresses will bend the material in any direction. Orientation measurements by means of microwaves showed chain orientations in the extrusion direction of the material and confirmed the assumption. Shrinking tests also confirmed the orientations.

Figure 6: Curve Characteristic of Internal Orientations

Conclusion

The development of a measurement technique to enable thermoformers characterizing their used material has been shown and proved by a laboratory device. The measurement technique was set up on a universal testing machine and can, within the project, be applied to a real measurement device suitable for material characterization. Further, several influences, such as draw ratio as well as plug diameter and clamping diameter, need to be investigated.

The parameter generation for simulation software like T-Sim is enabled through the reverse-engineering method. This method already exists but has to be automated within the project. An implementation of the method into the whole measurement apparatus as an add-on is planned.

Material quality control is possible as proved in case of additives and orientations or internal stresses in polymeric sheets. These results are only a first estimation and a more thorough investigation will take place within the project. Several processing, additive, thickness, heating time, crystallisation and friction influences will be investigated and provided with the final version of the apparatus.

References

- Ehrenstein, G.: Polymer-Werkstoffe, Hanser publisher, 2nd Edition, 1999

- Eyerer, P.: Einführung in die Kunststoffkunde, lecture script 2002.

- Kouba, K., Novotny, P., Kech, A.: Viscoelastic Material Characterization At Large Deformation, ANTEC 2001, Dallas, USA.